TECHNICAL SPECIFICATION

FOR RECOATING AND REPAIR OF ELECTROLYSER ELEMENTS TYPE UHDE BM2.7 GENERATION 4A

Scope of supply :

Recoat and mechanical reparation of Anodes half-shells and Cathodes half-shells type BM2.7 v4a belonging to ANWIL and in operation in the chlor-alkali plant in ANWIL Site

Cell Technical Parameters

Cell model: UHDE bipolar, natural circulation

Model BM 2.7 – 142

Membrane type: High-Performance

Membrane active area: 2.72 m²

Anode material: titanium, distributor: titanium / 0.2% palladium

Anode electrode type: Louver

Anode active layer: precious metals

Cathode material: nickel

Cathode electrode type: mesh

Cathode active layer: precious metals

- Technical scope of supply

- Recoating of anodes BM2.7 gener. 4a

- Incoming inspection, all process steps and repair work will be documented.

- Preparation of the electrode.

- Recoating procedure with LZM anode coating for 8 years at max. 6 kA/m².

- Removal of oxide layer in the contact areas.

- Leak-test.

- Straightening of the anode half-cell (basis: specification for new half-cells)

- Final quality check (basis: specification for new half-cells)

- Packing the anode half-cells into existing boxes, in case the existing packing is not re-usable, a new one will be prepared.

- Recoating of cathodes BM 2.7 gener. 4a

- Incoming inspection, all process steps and repair work will be documented

- Preparation of the electrode.

- Recoating procedure with HUH cathode coating for 8 years at max. 6 kA/m²

- Removal of oxide layer in the contact areas.

- Leak-test

- Straightening of the cathode half-cell (basis: specification for new half-cells)

- Final quality check (basis: specification for new half-cells)

- Packing the cathode half-cells into existing boxes, in case the existing packing is not re-usable, a new one will be prepared.

- Repair of anodes and cathodes BM 2.7 gener. 4a

- Incoming inspection, all process steps and repair work will be documented.

- Necessary mechanical repair work.

- Final quality check.

- Purchase specification

Terms and methods of preparation for the frame contract offer:

- Technical description of supply and realization method which will allow to judge the compatibility of the offer with the detailed scope of work.

- Technical references: The installer should provide documentation  on previous installations at similar chemical, petrochemical plants.

- Presentation of workers capabilities, hardware resources and associated certificates.

- The lifetime warranty will be 8 years for the anode and cathode coating. For the mechanical work shall be 24 months.

- The offer should include list of the cost of recoating procedure, mechanical repair work, packing and reshipment.